Micro-Topping by Concrete Coatings Inc. is a Concrete Micro-Topping for resurfacing existing interior and exterior concrete slabs. Micro-Topping transforms substandard concrete slab surface to a desired surface that can be a standalone finish or able to accept topical finishes. Durable enough for commercial, industrial and residential applications including showrooms, retails space and warehouses.

SECTION 035319

CONCRETE MICRO-TOPPING

PART 1		GENERAL

1.1	SUMMARY

A.	This Section specifies an applied micro-topping for horizontal cast-in-place concrete surfaces.

B.	Related Work:   Section 033000-  Cast-in-Place Concrete.

1.2	SUBMITTALS

A.	Product Data: Submit manufacturer’s product data and installation instructions.

B.	Applicator’s Project References: Applicator shall submit a list of successfully completed concrete topping projects, including project name, location, type, quantity of materials applied and name of architect.

1.3	QUALITY ASSURANCE

A.	Manufacture: Minimum 10 years experience producing concrete coatings.

B.	Applicator: Licensed applicator/installers, experienced and trained in the use of these products.

C.	Mock-Up if Required by Architect:  Construct on-site mock-up of concrete micro-topping in a location designated by the Architect, minimum 4 by 4 foot size. Receive approval of mock-ups by Architect for patterns, colors, textures, finishing, sealing, special effects and workmanship before application of permanent micro-topping overlay.

1.4	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials to site in original unopened factory labeled packaging with clearly identify name and manufacture.

B.	Store in a clean, dry area indoors. Store materials out of direct sunlight. Keep materials in manufactures original, unopened container and packaging until application. Use materials within manufacture’s recommended shelf life, approximately 12 months.

PART 2	PRODUCTS

2.1	MATERIALS

A	Concrete Micro-topping: Micro-Topping by Concrete Coatings Inc. 1105 North 1600 West, Layton, UT 84041, 800-443-2871, www.concretecoatingsinc.com

1.	Type: Cementitious Micro-Topping RG Natural which bonds to existing concrete.

2.	Type: Cementitious Micro-Topping SG which bonds to Micro-topping RG or G-100 Professional Grout Mix.

3. 	Coverage:  Approximately 200 to 400 square feet per 40 pound bag.

4.	Color: White.

5.	Color: Gray.

B.	Overlay Liquid Colorant for Integral Color: Integral Colorant by Concrete Coatings Inc.

C	Concrete Micro-Topping Sealer: Sealer by Concrete Coatings Inc.

1.		Type: CCI SuperSeal 2000 599 VOC.

2.	Type: CCI GemKote High Gloss Sealer meets 100, 350 and 400 VOC.

3.		Type: CCI Shield 50 100% solids, 100% cross linking epoxy, straw color.

4.		Type: CCI UV Shield 100% solids, 100% cross linking epoxy, water clear color.

PART 3	EXECUTION

3.1	PREPARATION

A.	Inspection: Prior to start of application, inspect existing conditions to ensure surfaces are suitable for installation including the following.

1.	Concrete has cured for a minimum of 28 days prior to application of overlay.

2.	Surface is completely free of sealers, oils, dirt, paint, penetrating sealers and foreign materials that would prevent the overlay from bonding to the concrete surface.

3.	Repair damaged and deteriorated concrete.

4.	Fill cracks, holes, spalls and low areas.

5.	Concrete has been cleaned per manufacture requirements.

B.	Protect all surrounding areas, walls, windows, landscaping and other adjacent surfaces from the execution of each item of work including but not limited to, surface preparation and all application steps of the cementitious micro-topping installation.

3.2	APPLICATION

A.	General: Following all manufacturers’ directions, as published in their product technical data sheet and installation guidelines regarding the application of the decorative cementitious micro-topping system.

B.	Substrate Conditioning: Dampen substrate with potable water. Maintain substrate at saturated surface dry (SSD) condition with no standing water or puddles during the placement of the base coat.

C.	Priming: Not required for the installation. Base coat of the cementitious resurfacing material (Micro-topping RG) must be applied to an SSD surface.

D.	Cementitious Micro-topping: Apply in strict compliance with manufacturer’s installation guidelines. Mix and spread micro-topping material onto substrate with recommended trowels and squeegees.  Apply in multiple coats as specified herein. A wet edge must be maintained at all times while placing mixed cementitious resurfacing material.

E.	Sanding: Sand between coats of micro-topping SG using methods prescribed in technical data sheet prior to staining or dying.

F.	Burnishing if Required: The final coat of micro-topping SG shall be burnished using a pool trowel, finish trowel or an acceptable method approved by Architect.

G.	Finish: Apply the specified finish per manufacturers instructions.

H.	Sealer: Strictly comply with manufacturer’s installation recommendations. Apply after finish has dried/cured at rate recommended by manufacturer. Clean surface as recommended by manufacturer.

3.3	CLEANING AND PROTECTION

A.	Protection: Do not cover.  Protect all completed work during the specified cure time of the material. Protect from contamination, vehicular or pedestrian traffic, and exposure to solid or liquid spills.  Do not allow tape or adhesives to be placed on materials until fully cured.

END OF SECTION