High-Performance, Stamp-Tek Stampable Overlay by Concrete Coatings Inc. is a stamped concrete overlay for resurfacing and texturing existing concrete slabs.  Stamp-Tek can transform an ordinary concrete surface into an elegant textured surface and is durable enough for commercial applications including restaurants, pool decks, showrooms and retail spaces. CCI SuperSeal 2000, CCI GemKote or 20WB protect Stamp-Tek stamped concrete, producing a high-gloss appearance.

SECTION 035322

STAMPED CONCRETE OVERLAY

PART 1	GENERAL

1.1	SUMMARY

A.	This Section specifies a stamped concrete overlay for resurfacing and texturing existing concrete slabs.

B.	Related Work:   Section 033000- Cast-in-Place Concrete.

1.2	SUBMITTALS

A.	Product Data: Submit manufacturer’s product data and installation instructions.

B.	Representative Samples: Submit manufacturer’s samples of standard colors.

1.3	QUALITY ASSURANCE

A.	Manufacturer: Minimum 10 years experience producing concrete coatings.

B.	Installer: Licensed installers experienced and trained in the use of these products.

C.	Mock-Up if Required by Architect:  Construct on-site mock-up of stamped concrete overlay in a location designated by the Architect, minimum 4 by 4 foot size. Receive approval of mock-ups by Architect for patterns, colors, textures, finishing, sealing, special effects and workmanship before application of permanent stamped concrete overlay.

1.4	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials to site unopened factory labeled packaging with clearly identifying name and manufacture.

B.	Store in a clean, dry area indoors. Store materials out of direct sunlight. Keep materials in manufactures original, unopened containers and packaging until application.  Use materials within manufacture’s recommended shelf life, approximately 12 months.

PART 2	PRODUCTS

2.1	MATERIALS

A.	Concrete Overlay: Stamp-Tek Stampable Overlay by Concrete Coatings Inc. 1105 North 1600 West, Layton, UT 84041, 800-443-2871, www.concretecoatingsinc.com

1.		Type: Cementitious concrete overlay which is stampable and bonds to existing concrete.

2.		Coverage:  Approximately 24 square feet at 1/4 inch thick per 50 pound bag.

3.	Color: White.

4.	Color: Gray.

B.	Reactive Primer: DuraSet VAE by Concrete Coatings Inc.

C.	Overlay Liquid Colorant for Integral Color: C Series Integral Colorant by Concrete Coatings Inc.

D.	Liquid Bond Breaker: Stamp-Tek Liquid Release by Concrete Coatings Inc.

E.	Stamping Mats: As selected by Architect and acceptable to Concrete Coatings Inc.

F.	Concrete Sealer:  Sealer by Concrete Coatings Inc.

1.	Type: CCI SuperSeal 2000 650 VOC.

2.	Type: CCI GemKote High Gloss Sealer, meets 100, 350 and 400 VOC requirements.

3.	Coverage: As Recommended by manufacturer.

PART 3	EXECUTION

3.1	PREPARATION

A.	Inspection: Prior to start of application, inspect existing conditions to ensure surfaces are suitable for installation including the following.

1.	Concrete has cured for a minimum of 28 days prior to application of overlay.

2.	Surface is completely free of sealers, oils, dirt, paint, penetrating sealers and foreign materials that would prevent the overlay from bonding to the concrete surface.

3.	Repair damaged and deteriorated concrete.

4.	Fill cracks, holes, spalls and low areas.

5.	Concrete has been cleaned per manufacture requirements.

3.2	APPLICATION

A.	Concrete Stamped Overlay: Strictly comply with manufacturer’s installation recommendations including the following:

1.	Use experienced installers.

2.	Protect adjacent areas from runoff, spills and tracking prior to application.

B.	Concrete Stamp Sealer: Strictly comply with manufacturer’s installation recommendations. Apply after Stamp-Tek has dried as recommended by manufacturer. Clean surface as recommended by manufacturer.

3.3	CLEANING AND PROTECTION

A.	Protection: Do not cover.  Protect all completed work during the specified cure time of the material. Protect from contamination, vehicular or pedestrian traffic, and exposure to solid or liquid spills.  Do not allow tape or adhesives to be placed on materials until fully cured.

END OF SECTION