Vivid™ Acid Stain by Concrete Coatings Inc. is a penetrating chemical stain which colors concrete surfaces with a beautiful variegated and mottled appearance.  Vivid Acid Stain can transform an ordinary concrete surface into the rich look of granite or marble, and is durable enough for commercial applications including restaurants, showrooms and retail spaces. CCI SuperSeal 2000 or CCI GemKote protect acid stained concrete, producing an attractive high-gloss appearance.

SECTION 099300

CONCRETE STAINING

PART 1	GENERAL

1.1	SUMMARY

A.	This Section specifies an applied stain and sealer for horizontal cast-in-place concrete surfaces.

B. 	Related Sections: Refer to the following specification sections for coordination:

1. 	Section 033000 - Cast-In-Place Concrete.

1.2	SUBMITTALS

A.	Product Data: Submit manufacturer's product data and installation instructions.

B	Mock-Up:  Prepare a test area minimum 2 by 2 feet in size to verify suitability of the stain, sealer and final appearance.

1.3	QUALITY ASSURANCE

A. 	Manufacturer: Minimum 10 years experience producing concrete coatings.

B.	Installer:  Licensed installers, experienced and trained in the use of these products.

C.	Suitability of Substrate:  Do not apply to concrete surfaces which may have insufficient chemical reaction, including older or weather concrete, concrete subject to runoff or weathered concrete, or heavily sandblasted concrete.

C.	Regulatory Requirements: Comply with requirements of authorities having jurisdiction and applicable codes at the location of the project.

1.4	DELIVERY, STORAGE AND HANDLING

A.	Deliver materials and products in unopened factory labeled packages. Protect from damage.

B. 	Store in a safe place, out of direct sunlight.  Keep containers tightly sealed.  Do not allow product to freeze.  Use within manufacturer’s recommended shelf life, approximately 12 months.

PART 2 - PRODUCTS

2.1	MATERIALS

A.	Concrete Stain:  Vivid Acid Stain by Concrete Coatings Inc., 1105 North 1600 West, Layton, UT 84041, 800-443-2871, www.concretecoatingsinc.com.  The concrete stain shall have the following properties:

1.	Type:  Penetrating chemical stain which chemically reacts with concrete.

2. 	Stain Colors:  Jade, Turquoise, Coffee, Amber, Mahogany, Ebony, Mission Brown, Caramel, Olive, Walnut and Weathered Terracotta.  Note that Turquoise and Jade colors are not suitable for slab concrete or areas subject to water from the sub-grade or standing water.

3.	Coverage:  200-300 square feet of concrete surface per gallon.

B.	Concrete Sealer:  Sealer by Concrete Coatings Inc., 1105 North 1600 West, Layton, UT 84041, 800-443-2871, www.concretecoatingsinc.com.

1.	Type:  CCI SuperSeal 2000, 650 voc.

2.	Type: CCI GemKote  High Gloss Sealer, meets 100, 350 and 400 voc requirements.

3.	Coverage:  As recommended by manufacturer.

PART 3 - EXECUTION

3.1	PREPARATION

A.	Inspection:  Prior to start of application, inspect existing conditions to ensure surfaces are suitable for installation including the following:

1.	Concrete has cured for a minimum of 28 days prior to application of stain.

2.	Surface is completely free of sealers, oils, dirt, paint, alkali, penetrating sealers and foreign materials that would prevent the stain from penetrating the concrete surface.

3.	Concrete has been swept clean.

4.	Test area has been approved.

3.2	APPLICATION

A.	Concrete Stain:  Strictly comply with manufacturer’s installation recommendations including the following:

1.	Use experienced installers wearing protective clothing and breathing apparatus.

2.	Test surface for suitable reactivity.

3.	Protect adjacent areas from over-spray, runoff, spills and tracking prior to application.

4.	For areas requiring material from more than one container, mix together prior to application to avoid color variation.

5.	Apply at rate recommended by manufacturer.

6.	Clean, rinse and neutralize surface.

B.	Concrete Sealer:  Strictly comply with manufacturer’s installation recommendations. Apply after stain has dried at rate recommended by manufacturer. Clean surface as recommended by manufacturer.

3.3	CLEANING AND PROTECTION

A.	Protection:  Do not cover, but protect floor area from paint and other contaminates that could inhibit the stain.

END OF SECTION